TECHNICAL DATA SHEET

La Casa dei Sogni

sect. 1.0 Technical characteristics

La Casa dei Sogni is a paint that stirs your Emotions. Its very application is brimming with charm, owing to the creative and personal content you will have to add to your every move when applying it. May I suggest you listen to some good music and follow the rhythm when you apply it in order to add art and spirit to the simple coloured matter.

sect. 2.0 Use

La Casa dei Sogni can be used on all suitably insulated surfaces.

sect. 3.0 Preparing the surface

Preparing the primer is vital to the success of the coating. Using Primus Sabbia is therefore indispensable.

sect. 4.0 Application method

La Casa dei Sogni is ready for use. Depending on the instructions on the sample collection, add your chosen COLOURING AGENT and mix by hand. Primus: Apply Primus Sabbia with a roller. Application: Soak our woollen glove generously in the paint. Start to distribute the product all over the wall with a casual movement of the palm of your hand. Keep the tip of the gloves “light”. If you wish your work to appear more “aged”, go over it lightly with the dampened glove after 15-30 minutes, creating a genuine mottled effect. If you wish to achieve a more uniform effect, reapply the same product.

sect. 5 Protective finish

Vetro: The product is ready for use. Leave the surface to be treated to dry for at least 48 hours. Apply 1 or 2 coats with a brush or roller. Output: 8/10 m2 with 1 litre

sect. 6.0 Technical characteristics: application

| Dilution/Mixing | Ready for use |
| --- | --- |
| Consumption | 0.20 ÷ 0.3 kg/m2 |
| Tools for application | Giorgio Graesan woollen glove |
| Primer | Primus Sabbia |
| Protective coating | Vetro |
| Application temperature | The ambient temperature must be between a minimum of +5°C and a maximum of +30°C while the relative humidity must be less than 85%, also for at least 24 hours after application. |

sect. 7.0 Technical characteristics: the product

| Composition | Water, breathable polymers. |
| --- | --- |
| Specific weight | 1.00 – 1.05 kg/l |
| pH after 30 days | 6.2 – 7.5 |
| Viscosity | Brookfield 20000 - 50000 cps |
| Storage temperature | Temperature of between +5°C and +30°C. Keep away from extreme cold. |
| EU VOC limit value for this product (cat. A/I): 300 g/l (2007) 200 g/l (2010) | 20 g/l white |
|  | 40 g/l coloured with our colouring agents |
| Colours available | As per our catalogue |
| Pot sizes | 0.75 – 2.5 – 5 litres |
| Warnings | There are no known cases of health hazards attributable to the product. Nonetheless, we recommend you observe the normal rules of industrial hygiene. In the event of accidental spillage, cover with soil or inert material. Collect most of the product and get rid of any residue with a water jet. |

sect. 8.0 Toxicological data

This product does not require any hazard labels pursuant to directives 67/548/EEC and 1999/45/EC and subsequent amendments and supplements.