TECHNICAL DATA SHEET

Colore & Gioia

sect. 1.0 Technical characteristics

Colore & Gioia is a decorative paint with iridescent effects. Thanks to the flakes of silver mother-of-pearl, the applied product reacts to light, changing its reflections according to the different lighting. This product affords good washability, is anti-bacterial and makes for countless application possibilities.

sect. 2.0 Use

Colore & Gioia is suitable for decorating indoor wall surfaces.

sect. 3.0 Preparing the surface

Preparing the primer is vital to the success of the coating. It is therefore advisable to trim and insulate properly before use, and to apply Primus Naturale or Primus Sabbia (as specified in the application method), which guarantee optimal grip and absorbency of the product.

sect. 4.0 Application method

Colore & Gioia is ready for use. Introduce the quantity of COLOURING AGENT specified in the catalogue and mix until the shade obtained is completely even. The product can be applied in 2 coats with a brush, a glove or a short-haired roller. Our Primer should be applied to prepare the surface to be coated. 2 coats of Primus Sabbia applied with a roller for subsequent brush or glove application. 1 coat of Primus Naturale for roller application. Only for applications on bathroom tiles with little joint, once thoroughly clean, at least two coats of Colore & Gioia can be applied directly onto the surface.

sect. 5 Protective finish

Vetro: When the product is applied with a roller over Colore & Gioia, there is no need to dilute it. It affords good coverage, water-resistance and complete washability of the wall. This protective coating must be applied over the tiles.

sect. 6.0 Technical characteristics: application

| Dilution/Mixing | Ready for use |
| --- | --- |
| Consumption | 100/150 g/m2 |
| Tools for application | Paintbrush, Glove, Short-haired roller |
| Primer | Primus Sabbia or Primus Naturale |
| Protective coating | Vetro |
| Application temperature | The ambient temperature must not be less than +5° C. Do not apply onto hot surfaces or those exposed to sunlight. |
| Drying time | The drying time varies between 6 and 8 hours |

sect. 7.0 Technical characteristics: the product

| Composition | Water, additives, mother-of-pearl flakes. |
| --- | --- |
| Specific weight | 1.10 kg/l |
| pH after 30 days | > 8-8.5 |
| Viscosity | > between 10000 and 12000 cps (Brookfield) |
| Storage temperature | Store in a sealed pot at a temperature of more than +5° C. Keep away from extreme cold. |
| EU VOC limit value for this product (cat. A/I): 300 g/l (2007) 200 g/l (2010) | Max content VOC 33 g/l |
| Colours available | As per our catalogue |
| Pot sizes | 1 – 2.5 – 5 litres |
| Warnings | If inhaled: Take the patient to a well ventilated location. Contact with eyes: rinse immediately with plenty of running water for at least 10 minutes. Skin contact: wash with running water; avoid prolonged contact. |

sect. 8.0 Toxicological data

The material is not labelled as irritating. There are no known effects on the eyes and skin.