TECHNICAL DATA SHEET

------------------------ PRIMUS AGGRAPPANTE------------------------

sec. 1.0 Technical characteristcs

PRIMUS AGGRAPPANTE is a levelling base, made of special resins in water base.

sec. 2.0 Use

Primus Aggrappante is suitable for indoor, as a smoothing material for tiles and a base for the application of Segui il tuo Istinto.

sec. 3.0 Preparation of the surface

A good preparation and cleanliness of the surface is essential for the optimal realization of the application. It is therefore necessary that the surface is dry, clean and dust free.

sec. 4.0 Application method

Primus Aggrappante is ready to use. Clean and degrease well the surface, apply one coat of Primus Aggrappante using our toothed trowel ( Kit/I ) which is advisable to use the ideal quantity of the product. Let the surface dry for around 24 hours before to apply “ISTINTO”.

sec. 5.0 Technical characteristics: application

| Dilution/Mixing | Ready to use |
| --- | --- |
| Consumption | 0,6 lt/m2 |
| Tools for application | Inox trowel (Kit/I) |
| Application temperature | Temperature must not be lower than +5° C. Do not apply on warm or insolated sufaces. |
| Drying time | 24 hours |

sec. 6.0 Technical characteristics: the product

| Composition | Smoothing base for tiles, resins in water dispersion |
| --- | --- |
| Specific weight | 1,70-1,90 Kg/l |
| pH after 30 days | 7,5-8,5 |
| Storage temperature | Store in a sealed pot at a temperature of more than +5° C. Keep away from extreme cold. |
| EU VOC limit value for this product: 30g/l l(2010) di C.O.V. | 0,17 g/l grey colour |
|  | 30 g/l voc max |
| Colour | Grey sand |
| Pot size | Lt 5 – Lt 2,5 |
| Warnings | If inhaled: Take the patient to a well ventilated location. Contact with eyes: rinse immediately with plenty of running water for at least 10 minutes. Skin contact: wash with running water; avoid prolonged contact. |

sec. 7.0 Toxicological data

This product requires Xi R41 labelling (irritating to the eyes and skin).