CONSOLIDATING FIXATIVE

DESCRIPTION

CONSOLIDATING FIXATIVE is a product to be use as a preparation for the application of Crazystone. To help the consolidation of the substrate and assisting the application of crazystone by extending the working time.

CONSOLIDATING FIXATIVE can be used as a primer for interior and exterior wall surfaces .

# support - utilization

| TYPE OF SURFACE | PRELIMINARY TREATMENTS |
| --- | --- |
| Plasterworks | Coat of CONSOLIDATING PRIMER. |
| Old plasterworks | Coat of CONSOLIDATING PRIMER. |
| Concrete | Coat of CONSOLIDATING PRIMER. |
| Medium density | Coat of CONSOLIDATING PRIMER. |
| Plasterboard | Coat of CONSOLIDATING PRIMER. |
| Plaster | Coat of CONSOLIDATING PRIMER. |
| Plastic coating | Washing and coat of CONSOLIDATING PRIMER. |
| Tiles | Accurate sand and coat of CONSOLIDATING PRIMER. |
| Not mineral decorative finishing | Accurate sand and coat of CONSOLIDATING PRIMER. |

# applicaTION

Add 1 litre of acrylic fixative to 6 litres of water and apply by brush or roller.

Allow to dry for 6 hours before the application of “Primus Naturale primer”.

# STORAGE

The product maintains its properties for a period of 12months if protected from excessive heat and cold.

Storage temperature must be included between +5°C and +30°C. Protect from frost.

# SAFETY GUIDELINES

Avoid contact with skin and eyes. If contact occurs, rinse thoroughly with water. For more information consult the safety sheet.

# DIPOSAL

The product must be disposed in agreement with current regulations.

Empty containers to be sent to recycling plants.

# TECHNICAL SPECIFICATIONS

| Aspect applied | Matte sattin |
| --- | --- |
| Color | Liquid dense white |
| Packaging | 1 Litre |
| Tools for the application | Roller or brush |
| Specific weight | 1,45 ± 0,05Kg/l |
| PH | 8 ± 0,5 |
| Thepretical performance | 150 ÷ 200g/ m2 in 2 coats |
| Application temperature | Minimum temperature +10°C - Maximum temperature +30°C |
| Dry to the touch | 3 hours with environmental temperature a 20°C |
| Dry in depth | 48 hours with environmental temperature a 20°C |