TECHNICAL DATA SHEET

Primus

sect. 1.0 Technical characteristics

Primus is an acrylic-based paint which is an ideal primer for our finishes. Applying the first coat of our products is much simpler after our primers have been applied onto the surface first. They are breathable and non flammable.

sect. 2.0 Use

Suitable for the preparation of indoor wall surfaces for the application of decorative paint.

sect. 3.0 Application method

Remove all dirt from the wall. Then apply a coat of Primus with a roller. Primus Naturale is the ideal primer for the preparation of surfaces before applying Spatula Stuhhi and Spirito Libero. Primus Sabbia is the ideal primer for the preparation of surfaces before applying Casa dei Sogni, Colore & Gioia, Colore & Oro and White Paint.

sect. 4.0 Technical characteristics: application

| Dilution/Mixing | Ready for use |
| --- | --- |
| Consumption | 0.15 ÷ 0.2 l/m2 |
| Tools for application | Roller |
| Storage | In a cool, dry and well-ventilated place, away from sources of heat and from direct sunlight |

sect. 5.0 Technical characteristics: the product

| Composition | Acrylic resins, natural pigments |
| --- | --- |
| Specific weight of Primus Naturale | 1.53 kg/dm³ |
| Specific weight of Primus Sabbia | 1.56 kg/dm³ |
| pH after 30 days | 8 ÷ 8.5 |
| Viscosity | 14000 ÷ 15000 cps Brookfield (10 rpm at 25°C) |
| Storage temperature | Temperature of between +5°C and +30°C. Keep away from extreme cold. |
| Permeability to vapour | High (Reference Standard: UNI EN ISO 7783-2:2001) |
| VOC value | 20 g/l |
| Density of vapours | >1 (water) |
| Pot sizes | 2.5 – 5 – 15 litres |

sect. 6.0 Toxicological data

The product does not contain any heavy metals or toxic solvents. The product is not classified as hazardous and does not require any labels. It is not considered hazardous for transport and is not governed by any regulations. No specific protective devices are required, but the room needs to be well aired. Dispose of any site waste in accordance with the applicable regulations in force, in authorised dumps.