# VENETIAN POLISHED PLASTER

# DESCRIPTION

VENETIAN POLISHED PLASTER is a blade-applied wall coating based on slaked lime putty finely filtered and seasoned for at least 6 months and on natural inert charges.

Its environmental friendly formula is solvent free (0% VOC).

Easy to apply, it has excellent filling power and resists aggression by moulds and bacteria.

VENETIAN POLISHED PLASTER is suitable for decorative indoor wall surfaces. Perfectly stable over time, it ensures outstanding breath through properties thanks to its excellent permeability to water vapour .

# color range

VENETIAN POLISHED PLASTER  is offered in WHITE colour.

Check our color range on www.venetianplastershop.com.au

.

# NEW SURFACE APPLICATION

| TYPE OF SURFACE | PRELIMINARY TREATMENTS |
| --- | --- |
| Any Surface (except render) | Apply 1 coat of Undercoat Sealer before priming |
| Old plasterworks | Brushing, eventual power washing and a coat of CONSOLIDATING PRIMER. |
| Render/ Base coat render | Coat of PRIMUS NATURALE primer. |
| Medium density | Coat of PRIMUS NATURALE primer. |
| Plasterboard | Coat of PRIMUS NATURALE primer. |
| Plaster | Coat of PRIMUS NATURALE primer. |
| Concrete | Coat of PRIMUS NATURALE primer. |
| Polished lime finishing | Accurate sanding and a coat of PRIMUS NATURALE primer. |
| Washable paints | Coat of PRIMUS NATURALE primer. |
| Non-mineral decorative finishings | Coat of PRIMUS NATURALE primer. |
| Plastic coating | A coat of oil based primer then a coat of PRIMUS NATURALE primer. |

Note: Advanced Spirito Libero recommends that our entire range of lime based natural materials is used only by highly skilled or licensed tradespeople with extensive experience in this field. It is the responsibility of the applicator to understand the application method and the procedure involved ,in order to obtain a satisfactory outcome. Advanced Spirito Libero recommends that architects, builders and clients appoint only experienced applicators in the relevant lime-based materials to ensure they'll be able to deliver the same finish as per the sample shown.

Following the Australian Building Code we do not suggest the installation of this product inside the shower area.

As with any lime-based material this product may change the appearance over time due to the ageing process caused by weather conditions"
To slow down this process the use of siloxane impregnating sealer is recommended over time.

# APPLICATION CYCLE

VENETIAN POLISHED PLASTER  is ready to use.

FIRST COAT

It should be applied carefully to apply it evenly.

Once the first coat is applied, the process has to be complete within 48h.

SECOND COAT

Proceed when the first coat is dry, being careful to apply it evenly, to create a flat surface without creases, but not glossy, to form a suitable support for the third coat.

THIRD COAT AND POLISHING

Proceed when the second coat is dry. Polishing is performed during the drying stage.

The gloss is the result of pressing the steel blade to the coating surface.

PROTECTIVE FINISH

| INDOOR SURFACES |  |  |
| --- | --- | --- |
| PRODUCT | CONSUMPTION | APPLICATION |
| BEE’S WAX: CERA DEL VECCHIO | approximately 30 ÷ 50 g/m2 | Let the surface dry out for at least 48 hours, then spread a coat of wax with a soft sponge for about 1 m2 only (about 11 ft2), and continue the application until the wall doesn’t absorb anymore. Remove the excess of wax from the surface. After about 30 minutes to 2 hours, proceed to rub with a non-woven fabric cloth (TNT, tissue-non-tissue) or mechanic polisher. |

ENVIRONMENTAL CONDITIONS OF APPLICATION

The environmental temperature must be included between +10°C and +30°C with relative humidity lower than 85%, also in the 24 hours following the application.

# STORAGE

The product maintains its properties for a period of 24 months if protected from excessive heat and cold.

Storage temperature must be included between +5°C and +30°C. Protect from frost.

# safety guidelines

Avoid contact with skin and eyes. If contact occurs, rinse thoroughly with water. For more information consult the safety sheet.

# disposal

The product must be disposed in agreement with current regulations.

Empty containers to be sent to recycling plants.

# TECHNICAL SPECIFICATIONS

| Appearance | glossy, fine-grained, with natural shading |
| --- | --- |
| Packaging | 12 Kg net |
| Applications tools | Venetian Plaser trowel |
| Specific weight | 1,56 ± 0,05 Kg/l |
| Theoretical yield | 0,80 ÷ 1,00 Kg/m2 in 3 coats |
| Granulometry | impalpable |
| Coating thickness | 0,50 ÷ 0,65 mm in 3 coats |
| Dry to the touch | 3 hours with environmental temperature of 20°C |
| Dry to handle | 48 hours with environmental temperature of 20°C |
| Stable hardness | 180 days |
| Dry to recoat | 6 hours with environmental temperature of 20°C |
| pH after 30 days | 12,5 ± 0,2 |
| flammability | Non-flammable - Class A1 |
| Permeability to water vapour (Sd) | High 0,06m (Standard: UNI EN ISO 7783-2:2001) |