Description

Giorgio Graesan Consolidative Fixative is a product to be used as a preparation for the application of Giorgio Graesen Istinto, to help with the consolidation of the substrate and assist in the application of Istinto by extending the working time of the Istinto

Uses

Suitable for the preparation of indoor wall surfaces in readiness for the application of other Giorgio Graesan decorative wall coverings.

Can be applied over any standard building substrate following correct surface preparation

Colour White to off-white colour

Sheen Level Matt Satin

Coverage Rate 200 ml per m2 - 2 coats required

Application Method Roller or brush-Product is to diluted to a ratio of 100ml of fixative to 200 ml water

Typical Data at 25’C and 50% Relative Humidity

Drying Time 6 hours

Touch Dry 3 hours

Curing Time 48 hours

Usual No of Coats Two coats

Clean Up Water

Packaging Sizes 1 Litre

Abrasion Resistance Not applicable

Water Resistance

 Not applicable

Pot Life Once opened, use within 12 months. Store in a cool, dry and well ventilated place, away from sources of heat and from direct sunlight

Substrate Conditions

Substrate must be installed as per manufacturer’s specifications prior to application

Substrate must be clean and free of dust, dirt, oil, salt, mould or any other contamination

Any base coats should be fully cured

For full details on application for each substrate refer to the Giorgio Graesan Specification and System Guide

Mixing

Consolidating Fixative is pre mixed and comes ready to use. Product will need to be diluted and mixed thoroughly before use.

Application

Apply Consolidating Fixative with a roller or brush, ensuring full, even coverage of the surface area*.*

Precautions and Limitations

Adequate PPE should be used when mixing and applying product

Do not apply if the temperature will fall below 5’C or above 35’C during application.

Do not apply in direct sunlight, wind or rain and protect the finished work until fully cured

Transport and Storage

Store in a cool, dry place

Keep pail sealed when not in use

Disposal

Dispose of in accordance with local council regulations

Safety Data

Refer to Giorgio Graesan Consolidating Fixative Plaster SDS

Giorgio Graesan will not accept responsibility for any misuse of this product or if not applied by a skilled and experienced applicator and in accordance with our technical specifications. Due to our policy of continuing product improvement, Giorgio Graesan Australia reserves the right to change these specifications without further notice. Our goods come with guarantees that cannot be excluded under the Australian Consumer Law. You are entitled to a replacement or refund for a major failure and compensation for any other reasonably foreseeable loss or damage. You are also entitled to have the goods repaired or replaced if the goods fail to be of acceptable quality and the failure does not amount to a major failure.