Description

Giorgio Graesan Vetro is water based resin finishing coat that leaves a decorative brilliant effect to plastered walls. Vetro prevents the build up of dirt and makes the surface completely washable and weatherproof

Uses

Suitable for sealing of indoor wall surfaces that have had an application of other Giorgio Graesan decorative wall coverings.

Can be applied over any standard building substrate following correct surface preparation

Colour Clear Liquid

Sheen Level Matt or Satin

Coverage Rate 200 ml per m2 - 2 undiluted

Application Method Roller or brush

Typical Data at 25’C and 50% Relative Humidity

Drying Time 2 hours

Touch Dry 30 minutes

Curing Time 24 hours

Usual No of Coats 3 coats

Clean Up Water

Packaging Sizes 2.5Litre, 1 Litre

Abrasion Resistance Not applicable

Water Resistance Not applicable

Pot Life Once opened, use within 12 months. Store in a cool, dry and well ventilated place, away from sources of heat and from direct sunlight

Substrate Conditions

Substrate must be installed as per manufacturer’s specifications prior to application

Substrate must be clean and free of dust, dirt, oil, salt, mould or any other contamination

Any base coats should be fully cured

For full details on application for each substrate refer to the Giorgio Graesan Specification and System Guide

Mixing

Vetro is pre mixed and comes ready to use. Product will need to be mixed thoroughly before use.

Application

Apply Vetro with a roller or brush, ensuring full, even coverage of the surface *area.*

Vetro is to be applied in 3 coats allowing suitable drying time in between each coat

First Coat diluted 10% Vetro/90% water

Second Coat diluted 50% Vetro/50% water

Third coat undiluted 100% Vetro

Precautions and Limitations

Adequate PPE should be used when mixing and applying product

Do not apply if the temperature will fall below 5’C or above 35’C during application.

Do not apply in direct sunlight, wind or rain and protect the finished work until fully cured

Transport and Storage

Store in a cool, dry place

Keep pail sealed when not in use

Disposal

Dispose of in accordance with local council regulations

Safety Data

Refer to Giorgio Graesan Vetro Plaster SDS

Giorgio Graesan will not accept responsibility for any misuse of this product or if not applied by a skilled and experienced applicator and in accordance with our technical specifications. Due to our policy of continuing product improvement, Giorgio Graesan Australia reserves the right to change these specifications without further notice. Our goods come with guarantees that cannot be excluded under the Australian Consumer Law. You are entitled to a replacement or refund for a major failure and compensation for any other reasonably foreseeable loss or damage. You are also entitled to have the goods repaired or replaced if the goods fail to be of acceptable quality and the failure does not amount to a major failure.